BEES Please Product Summary: Forbo Industries Marmoleum Linoleum


BEES Please Product Summary
BEES Please Product:  Forbo Industries Marmoleum Linoleum

Product Selection and Description

Linoleum is a resilient, organic-based floor covering consisting of a backing covered with a thick wearing surface. Oxidized linseed oil and rosin are mixed with the other natural ingredients to form linoleum granules.  These granules are then calendared onto a jute backing, making a continuous long sheet.  The sheets are hung in drying rooms to allow the naturally occurring process to continue until the product reaches the required flexibility and resilience.  The sheets are then removed from the drying rooms, cut into rolls, and prepared for shipment.

Forbo Marmoleum may be installed using either a styrene-butadiene or a low-VOC adhesive. Both installation options are included in BEES. The detailed environmental performance data for these products may be viewed by opening the files C3020R.DBF (styrene-butadiene adhesive) and C3020NN.DBF (low-VOC adhesive) under the File/Open menu item in the BEES software.

The detailed environmental performance data for these products may be viewed by opening the following files under the File/Open menu item in the BEES software:

· C3020R.DBF—Marmoleum with Standard Adhesive

· C3020NN.DBF—Marmoleum with Low-VOC Adhesive

Flow Diagram

The flow diagrams below show the major elements of the production of this product as it is modeled for BEES. 

[image: image1.wmf]Functional Unit 

of 

Marmoleum

End

-

of

-

Life

Truck

Transport to

Bldg

Site

Forbo

Marmoleum

Flooring

Process energy

Transport by 

train

Limestone 

Production

Marmoleum

production

Adhesive

Production

Raw material 

transport

Sawdust 

Production

Wood 

Prod

’

n

& Harvesting

Transport by 

ship

Transport by 

truck

Tall oil 

Production

Linseed oil 

Production

Rosin 

Production

Jute 

Production

Pigment 

Production

Acrylic 

Lacquer 

Production

Flax seed 

Production

Agrichemicals

production

Fertilizer

production

Fertilizer

production


Figure 1: Forbo Marmoleum System Boundaries

Raw Materials

The table below lists the constituents of 2.5 mm (0.10 in) linoleum and their proportions.   

Table 1: Forbo Marmoleum Constituents

	Linoleum Constituents
	Mass Fraction (%)

	Mass per Applied Area  in g/m2 (lb/ft2)

	Linseed oil
	20
	588 (0.12)

	Tall oil
	13
	398 (0.08)

	Pine rosin
	3
	76 (0.02)

	Limestone
	20
	592 (0.12)

	Wood flour 
	31
	901 (0.18)

	Pigment
	4
	101 (0.02)

	Jute (backing)
	8
	233 (0.05)

	Acrylic lacquer
	1
	12 (0.00)

	Total:
	100
	2 901 (0.59)


The cultivation of linseed is based on a modified version of wheat production from the US LCI database (for lack of other available data).  To harvest the linseed, it is assumed that a diesel tractor is used – approximately 0.61 MJ (0.17 kWh) of diesel per kg (263 Btu/lb) of linseed harvested.  The yield of linseed is 1 038 kg per hectare (420 lbs per acre).  Energy requirements for linseed oil production include fuel oil and steam, and are allocated on an economic basis between linseed oil (87 %) and linseed cake (13 %). Allocation is necessary because linseed cake is a co-product of linseed oil production whose production impacts should not be included in the BEES model.  The emissions associated with linseed oil production are allocated on the same economic basis.  The production of the fertilizers and pesticides is based on elements of the SimaPro database. 

The production of tall oil is based on European data for kraft pulping, with inventory flows allocated between kraft pulp and its coproduct, tall oil.
  Pine rosin production is assumed to have no burdens, since the harvesting of raw pine rosin is done mainly by hand, according to Forbo.  

The production of limestone comes from the US LCI Database.  Wood flour is sawdust produced as a coproduct of wood processing, and its production is based on the CORRIM data found in the US LCI Database. 

Production of the pigments used is modeled based on the European production of titanium dioxide, from the SimaPro database.  Linoleum backing, jute, is mostly grown in India, Bangladesh, Thailand, and China.  Jute is a predominantly rain-fed and requires little fertilizer and pesticides, and cultivation is generally manual.  Data for the production of acrylic lacquer materials are based on elements of the SimaPro database.  

Manufacturing

Energy Requirements.  The production of each unit of Marmoleum (0.09 m2 or 1 ft2) requires 0.45 MJ (0.13 kWh) of electricity and 1.8 MJ (0.5 kWh) of natural gas.  The production and use of energy is based on the US LCI database.

Transportation.  Transportation distances for shipment of the raw materials from the suppliers to the manufacturing plant were provided by Forbo.  The materials were transported by diesel truck rail, and in some cases ocean freighter.  All of these transportation modes were accounted for and modeled, with data based on the US LCI database.

Transportation

The transportation distance from the manufacturing plant to the building site is modeled as a variable in BEES.  The product is shipped by diesel truck, which is based on data from the US LCI database.   

Installation 

The installation of Marmoleum may be done using 0.0003 kg (0.0007 lb) of either a styrene-butadiene or a low-VOC adhesive.  Additionally, an acrylic sealant is applied to the flooring for each installation.  Approximately 6% of the flooring is wasted during installation, and this is incorporated into the production and manufacturing aspects of the models.

Use Phase

Linoleum is known for its longevity.  Through evaluation of actual lifetime data, is has been determined that linoleum has a useful life of 30 years.
  As with all BEES products, the life cycle environmental impacts from this replacement are included in the inventory data.

End-of-Life

At the end of its life, the used flooring is sent to a landfill. 

References

Life Cycle Data

National Renewable Energy Laboratory (NREL): U.S. Life-Cycle Inventory Database. 2005. Golden, CO. Found at: http://www.nrel.gov/lci/database 

PRé Consultants: SimaPro 6.0 LCA Software. 2005. The Netherlands.

Marieke Goree, Jeroen Guinée, Gjalt Huppes, Lauran van Oers, Environmental Life Cycle Assessment of Linoleum (The Netherlands: Leiden University, 2000).

Fédération Européenne des Fabricants de Carton Ondulé (FEFCO), European Database for Corrugated Board Life Cycle Studies, 2003. Found at:  http://www.fefco.org/fileadmin/Fefco/pdfs/Technical_PDF/Corrected_database_2003.pdf

Federal Association of the Sworn Experts for Room and Equipment e.V., Guide to the Inquiry of Time Values and Decreases in Value of Floor Coverings, (Bonn, Germany: Federal Association of the Sworn Experts for Room and Equipment e.V.).

Industry Contacts

Tim Cole, Forbo Industries (2002)







� Marieke Goree, Jeroen Guinée, Gjalt Huppes, Lauran van Oers, Environmental Life Cycle Assessment of Linoleum (The Netherlands: Leiden University, 2000). 


� Fédération Européenne des Fabricants de Carton Ondulé (FEFCO), European Database for Corrugated Board Life Cycle Studies, 2003. Found at:  http://www.fefco.org/fileadmin/Fefco/pdfs/Technical_PDF/Corrected_database_2003.pdf


� Federal Association of the Sworn Experts for Room and Equipment e.V., Guide to the Inquiry of Time Values and Decreases in Value of Floor Coverings, (Bonn, Germany: Federal Association of the Sworn Experts for Room and Equipment e.V.).





